## Slide 1: 5-1700 Long-Term Performance of Portland Cement Concrete Pavement - Training Materials -
Center for Transportation Research
The University of Texas at Austin
March 2006

## Slide 2
Background
Concrete setting temperature (e.g., zero-stress temperature) has significant effects on CRCP performance.
Current specifications limit concrete temperature as delivered, not setting temperature.
There is a need to control concrete setting temperature in specifications.

## Slide 3
Shadow Specifications
Primary objective of shadow specifications is to control concrete temperatures during cement hydration phase.
Shadow specifications require the use of temperature prediction program as well as temperature measuring devices.

## Slide 4
Temperature Requirements in Shadow Specifications
The maximum concrete temperature for the first 24 hours after concrete placement shall not exceed 120°F.
Temperature difference between the top and the bottom of the slab for the first 48 hours after concrete placement shall be less than 25 °F.

## Slide 5
- Concrete Temperature Prediction -
■ Weather, materials & pavement structure
■ Temperature prediction at top, middle, & bottom of slab
Insert temperature
measuring devices
  - Preparation -
  ■ Temperature prediction model
  ■ Temperature measuring devices
If 120° F>Temp.
If 120° F<Temp.
■ Only two sets at the predicted time of maximum concrete temperature and temperature differential
■ Every hour in the morning
■ Every 2 hours after 12 p.m.
■ Maximum concrete temperature shall not exceed 120° F
■ Temperature difference between the top and the bottom of the slab shall be less than 25° F

## Slide 6
Temperature Predictions by PavePro

## Slide 8: PavePro - input variables -
General inputs
Mixture proportion
Materials
Environmental condition
Construction inputs

## Slide 9: General Inputs
Pavement structure
Reliability
Project information

## Slide 12: Mixture Proportion
Weight proportions of each ingredient

## Slide 14: Materials
Chemical composition & hydration properties of cementitious materials
Information on coarse aggregates
Default values provided

## Slide 17: Environmental Condition
Ambient temperature
Relative humidity
Wind speed
Cloud cover

## Slide 19
Environmental Input Source
http://www.srh.noaa.gov/ifps/MapClick.php?FcstType=digital&textField1=30.3153839111328&textField2=-97.7663345336914&site=ewx

## Slide 22: Construction Inputs
Fresh concrete temperature
Base course temperature
Curing method

## Slide 24
Temperature Predictions
- PavePro Output -

## Slide 28
Predicted Temperatures at Top
Austin US183 Test Section

## Slide 29
Predicted Temperatures at Middle
Austin US183 Test Section

## Slide 30
Predicted Temperatures at Bottom
Austin US183 Test Section

## Slide 31: Implementation of Shadow Specifications -Test Sections-
US 183 in Austin
US 290 in Austin
US 59 in Houston

## Slide 32
Austin US183 Test Section

## Slide 33
Austin US290 Test Section

## Slide 34
Cleveland US59 Test Section

## Slide 35
US 183 US 290 US 59
Pavement Structure of Test Sections

## Slide 36
Test Section | Unit | US183 | US290 | US59
W/C ratio Cement Factor Coarse Aggregate Factor Max. Aggregate Size Water Cement Coarse Aggregate Fine Aggregate Fly Ash Air Entraining Reducer Retarding | - Sk./cy - inch lbs/cy lbs/cy lbs/cy lbs/cy lbs/cy oz oz | 0.52 5.0 0.685 1.0 229 358 1916 1368 100 2.64 10.58 | 0.59 - - - - 336 1816 1287 152 - - | 0.44 5.5 0.740 Grade 2 215 362 1848 1265 131 0.83 4.14
Concrete Mix Design used on Each Test Sections

## Slide 37
Temperature Measuring Device
- I-Button Programming -

## Slide 38: I-Button

## Slide 39: I-Button Assembly
Solder
Wire
Coat
Assemble

## Slide 40: Long-Term Durability of I-Button Assembly
The integrity of the i-button assembly needs to be inspected prior to installation.
If i-buttons are not completely sealed, pore solutions in Portland cement concrete could cause electrical instability of the i-button assembly.
Testing is required to ensure the complete sealing of i-buttons.

## Slide 41
Testing Coating Integrity in a Salt Water Bath
Salt Water Bath
I-Button Assembly
Ohmmeter
~ 30k W = Short
> 30M W= Good

## Slide 42: Connection of I-Button Assembly to Data-Logger (Laptop Computer)

## Slide 43: I-button Software

## Slide 52
Installation of
I-Button Assembly

## Slide 53
I-Buttons

## Slide 56
I-button Data Downloading

## Slide 59
Processing of Downloaded Temperature Data

## Slide 60: Processing Downloaded Data
Open the file with Excel

## Slide 66
Graphic Presentation of Processed Downloaded Data from US 183 Test Section in Austin

## Slide 67
Actual Temperature at the Top

## Slide 68
Actual Temperature at the Middle

## Slide 69
Actual Temperature at the Bottom

## Slide 70: Compliance with Shadow Specifications Requirements
Inspect the maximum concrete temperature within 24 hours of concrete placement.
Inspect the maximum concrete temperature differential within 48 hours of concrete placement.

## Slide 71: Future Developments
Pay factors or disincentives for non-compliance
Further enhancement of temperature prediction models
Continued efforts to quantify the effects of concrete temperature on long-term CRCP performance