## Slide 1: Construction of Cast-in-Place Post-Tensioned Concrete Pavement Collection of Pictures
TxDOT Implementation Project 5-4035
Texas Tech University

## Slide 2
Notes: First phase: polyethylene sheet and armor joint placed. Gap slab shown between 14-in CRCP and 9-in PCP

## Slide 3
Notes: Gap slab between 14-in CRCP and 9-in PCP

## Slide 4
Notes: Placing transverse post-tensioning bar (1-in diameter at 6-ft spacing)

## Slide 6
Notes: Assembly of longitudinal tendons

## Slide 7
Notes: Assembly of longitudinal tendons

## Slide 8
Notes: Later on, they used machine to assemble longitudinal tendons – improved efficiency

## Slide 9
Notes: Cutting the tendon at the right length: early-stage practice

## Slide 10
Notes: Cutting the tendon at the right length: improved practice

## Slide 12
Notes: Close-up view of assembled dead end anchor

## Slide 13
Notes: The other end of longitudinal tendon assembly

## Slide 14
Notes: Tendons at stressing pocket locations

## Slide 15
Notes: Stressing pockets

## Slide 16
Notes: Stressing pocket installation

## Slide 17
Notes: Close-up view of stressing pocket (8-in wide x 48-in long)

## Slide 18
Notes: Stressing pockets with cover on

## Slide 19
Notes: Maturity meter (i-button) in place at the first transverse post-tensioning bar (direction of concrete placement from right to left, so that the strength estimate using maturity is somewhat conservative)

## Slide 20
Notes: Armor joint with anchor bars and stainless steel dowels along with grout tubes

## Slide 21
Notes: Initial joint opening (3/4 inches0

## Slide 22
Notes: First day of paving (May 27, 2008)

## Slide 23
Notes: Concrete placement started about 10-ft beyond the first armor joint, and the area between 14-in CRCP and this starting location was placed by hand

## Slide 24
Notes: Concrete placement by hand with forms on the side

## Slide 25
Notes: Vibration of concrete at the gap slab

## Slide 26
Notes: Tendons ready and concrete placement in progress

## Slide 27
Notes: Once the concrete paving started, there was not much difference in concrete placement between PCP construction and other PCC paving construction. Placer and spreader was used to supply concrete, and same type of slip form paver was used. The speed of the paver was comparable to or a little bit slower than that for normal PCC paving.

## Slide 28
Notes: Enough concrete in front of the paver

## Slide 29
Notes: On the first day, transverse reinforcements being pushed by concrete pressure

## Slide 30
Notes: Contractor trying to hold transverse steel while the paver is approaching

## Slide 31
Notes: Contractor came up with the idea of placing longitudinal steel and tie transverse reinforcements to the longitudinal steel. This helped a little in preventing transverse reinforcements being pushed.

## Slide 32
Notes: Later, the contractor used bars that they hammered into the subbase, in addition to longitudinal steel described in the previous slide, to hold transverse post-tensioning bars. A total of four bars were driven into the subbase per transverse post-tensioning bar. These bars, however, were installed every third transverse post-tensioning bar. This practice needs further evaluation since the bars will restrain concrete volume changes and could result in pre-stress loss.

## Slide 33
Notes: With all the efforts to keep the reinforcements in place during concrete placement, undulations in longitudinal tendons are observed.

## Slide 34
Notes: Working on stressing pockets – quite labor intensive

## Slide 35
Notes: Locating pockets for transverse post-tensioning bars assembly

## Slide 36
Notes: Edge failure at the transverse post-tensioning bars assembly

## Slide 37
Notes: Little difference in finishing operations from those for normal PCC pavements, even though it was stated that the finishers were able to “feel” as if the slab was moving while they were finishing with straight-edge (apparently due to plastic sheet underneath).

## Slide 38
Notes: Carpet drag operation – no difference from normal concrete paving

## Slide 39
Notes: Tining operations are the same. Grout hoses are shown for transverse post-tension bars

## Slide 40
Notes: No difference in curing machine operations

## Slide 41
Notes: Good curing

## Slide 42
Notes: Checking the maturity to estimate compressive strength for the time of initial post-tensioning

## Slide 43
Notes: Steel piece that holds the armor joint is removed before the initial post-tensioning is applied.

## Slide 44
Notes: Locating grout hoses chipping concrete to expose grouting hoses at armor joint

## Slide 45
Notes: Initial post-tensioning

## Slide 46
Notes: Initial post-tensioning (target: 15 kips per tendon)

## Slide 47
Notes: Post-tensioning for transverse post-tensioning bar (target: 46.6 ksi per bar)

## Slide 48
Notes: Measuring the extension of transverse bar during post-tensioning operation

## Slide 49
Notes: CRCP gap slab

## Slide 50
Notes: Contractor looking at the sheet to determine how much post-tensioning force he has to apply. This table was to address low strength due to cold temperature. The numbers in the far right column are the pressure they will go by on the gage in slide 46.

## Slide 51
Notes: A transverse crack was observed on the slab placed on Aug 4, 2008. The crack was near the center of the slab.

## Slide 52
Notes: Longitudinal crack was also observed on the slab placed on August 4, 2008.

## Slide 53: Instrumentation

## Slide 54
Testing Setup

## Slide 55
VWSG
RH Gages
Stressing Pockets
Additional
VWSG location
Additional
VWSG location
Notes: Over view of gages installed

## Slide 56
Notes: Vibrating wire strain gages placed in longitudinal and transverse directions, also at different depths

## Slide 57
Notes: Relative humidity sensors at different depths

## Slide 58
Notes: Slab displacement gages installed along the edge of the slab

## Slide 59
Notes: Connecting wires to data logger

## Slide 60
Data Logger
Notes: Semi-permanent data logger